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TESt report

Customer



Tester
Date
28.10.2025

TEST METHOD
Abrasion resistance, Martindale


Determination of specimen breakdown
Standard

SFS-EN ISO 12947-2:2016

Nominal pressure

kPa
Pretreatment
Standard atmosphere (ISO 139: RH65%, T20°C)

Testing conditions
Standard atmosphere (ISO 139: RH65%, T20°C)
Observation method
Microscope (>10 x magnification)
Test interval


rubs

Foam backing
Yes

Material details according to the information provided by the customer:


MATERIAL

Specimens
1. Ahlstrom nonwoven


2.
Ahlstrom nonwoven


	Rubs
	Observations

	1000
	1st layer coming off both samples. Sample 1 worse than sample 2

	2000
	Abrasion around edges becoming worse

	3000
	Increased pilling, 2nd layer coming off 

	4000
	Both are becoming more open

	5000
	Both look like only 

	6000
	

	7000
	

	8000
	


According to standard the results are reported as the number of rubs before the specimen breakdown have been occurred. The final result is the lowest individual result.
Results
	Specimen
	1.
	2.
	Result

	[Rubs]
	
	
	


End point acc. to standard: Hole equal to 2,5 mm
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